Fate Determination and Characterization of Food Additive Silicon Dioxide and Titanium Dioxide in Commercial Foods

Ri-Ye Kwon1, †, Su-Bin Kim1, †, Su-Min Youn1, and Soo-Jin Choi1,*

1Division of Applied Food System, Major of Food Science & Technology, Seoul Women’s University, Seoul 01797, Republic of Korea

*Correspondence: sjchoi@swu.ac.kr; Tel.: +82-2-970-5634

†These authors contributed equally.

Table S1. Operating conditions of the ICP-AES instrument

| Instrument parameter | Operating conditon |  |
| --- | --- | --- |
|  | SiO2 | TiO2 |
| RF(radio frequency) power (W) | 1000 | 1300 |
| Gas flow (L/min) | 12 | 12 |
| Nebulizer flow (mL/min) | 0.75 | 0.75 |
| High voltage (V) | 990 | 650 |
| Wavelengths (nm) | 212.412 | 334.941 |

Figure S1. (A) Transmission electron microscopy (TEM) images and (B) size distribution of pristine food additive SiO2 and TiO2. Size distributions were obtained by randomly selecting 100 particles from the TEM images. (C) Zeta-potentials of SiO2 and TiO2 suspension as a function of pH.